## Slide 1
Design Temp | User | Material Std | User |  | Insulated | User
Design Pressure Psi (P) | User | Material Grade | User |  | Insulation Type | User
Operating Temp | User | PWHT | User |  | Nom Dia (D) inches | User
Operating Pressure | User | Corrosion allowance(CA) | User |  | Nom Thk- inches | User
Pipe Spec | User | User calculated Min Thk (UMT) | User | N | Length- inches | User
Joint Efficiency(E) | User | Pr Min Req Thk-Int (PMT) | See below | N | MDMT Temp | User
Construction Code | User | Struc Min Thk (SMT) | Master table |  | Effective MT (EMRT) | See logic below
Allowable Stress (S) | From material table (user can type in also) | Yield Strength (YS) | From material table (user can type in also) |  | Tensile Strength (TS) | From mate rial table (user can type in also)
Flow Stress | See logic below | Pr Min Req Thk-Ext (PMT-E) | - |  | Strength Ratio | See Logic Below
 |  | Last measured Year (LMY) | TML table | N | Effective Thk | See logic below
 |  | Last measured Thk (LMT) | TML table |  |  | 
Design Data Tab
Effective Min thk (EMRT) :
If UMT is “Y” then EMRT=UMT
Elseif PMT is “Y” then EMRT= Max (PMT , SMT)
Elseif CA is null then EMRT= Nom Thk*0.9
Elseif CA is not null EMRT= Nom Thk- CA
Pr Min Thk (PMT): (P*D/2(SE-0.6P)
P = Design Pressure in PSI
D = Dia in inches
S= Allowable Stress
E= Efficiency
Flow Stress
((YS+TS)/2)*1.1*E
Strength Ratio
(S*E*EMRT)/(FS*ETHK)
Effective Thk:
If LMIY =Y then Effective Thk= LMIT
Else Effective Thk= Nom Thk

## Slide 2
Injection points/ Intermitent | N | Theoretical corrosion rate (TICR) | From Corr study table | Y | Inspection confidence (Heading) | 
Effective I Corrosion Rate | See logic below | Measured long term CR (LICR) | TML table | N | Very High | From Insp Confidence table
Damage Factor | POF IC | Measured Short term CR (SICR) | TML table | N | High | From Insp Confidence table
POF | POF IC | Effective Internal Age | See logic below |  | Med | From Insp Confidence table
 |  |  |  |  | Low | From Insp Confidence table
Internal corrosion Tab
Effective Internal Corrosion Rate (EICR):
If LICR =Y then EICR=LICR
elseIf SICR =Y then EICR=SICR
elseIf Injection point =Y then EICR=2* TICR
elseIf Injection point =N then EICR= TICR
Effective Internal Age:
If LMY =Y then AGE=Present Year-LMY
Else AGE= Present Year-YIS

## Slide 3
Soil Interface/Condensation | N | Theoritical corrosion rate (TECR) | From external corrosion table/CUI table (EC- 15.2 & CUI 16.2/16.3), Corro Study | Y | Type of Corrosion (External/ CUI/Process) | 
Pipe direct on beam/ complex design | N | Measured long term CR (LECR) | TML table | N | Very High | From Insp Confidence table
Coating Quality- CQ(H/M/L) | M | Measured Short term CR (SECR) | TML table | N | High | From Insp Confidence table
EC driver (climate) M/T/D/S | M |  |  |  | Med | From Insp Confidence table
Coating age (COATAGE) | (Present Year-RPY) |  |  |  | Low | From Insp Confidence table
Coat Adjustment | See logic below | Effective Ex CR (EECR) | See logic below |  | Found | From Insp Confidence table
Repainted Year (RPY) | Pipe reports | Line ex Age (LEAGE) | If LMT=Y then Present year-LMY else Present Year-YIS |  | Damage Factor | POF EC table
Effective External Age | LEAGE-COatAdjust | External Process | from Corrosion Study table (default “atmos”) |  | POF | POF EC table
External/ CUI/ Process corrosion data
Effective External Corrosion Rate (EICR):
If LECR =Y then EECR=LICR
elseIf SECR =Y then EECR=SECR
elseIf Soilinterface or/and Pipe direct =Y then EECR=2* TECR
Else EECR= TECR
Coating Adjustment
If LEAGE>= COATAGE and CQ=L then 0
else if LEAGE>= COATAGE and CQ=M then min of( 5 or COATAGE)
else if LEAGE>= COATAGE and CQ=H then min of( 15 or COATAGE)
else if LEAGE< COATAGE and CQ=L then 0
else if LEAGE< COATAGE and CQ=M then (min of( 5 or COATAGE)-min of(5, (coatage-LEAGE)
else if LEAGE< COATAGE and CQ=H then (min of(1 5 or COATAGE)-min of(15, (coatage-LEAGE))
If “external process” = “Atmos” and “material code” starts with “CS” or “LAS” and “Insulated”=“N” then “Type Of Corrosion” = “External” and TECR from table 15.2
If “external process” = “Atmos” and “material code” starts with “CS” or “LAS” and “Insulated”=“Y” then “Type Of Corrosion” = “CUI” and TECR from table 16.2 and 16.3
If “external process” not equal to “Atmos” then “Type Of Corrosion” = “Process” TECR from corrosion study table and the TAB is replaced by ‘Internal Corrosion Tab”

## Slide 4
Coating Quality- CQ(H/M/L) | M | Susceptibility | Table 17.2 / Table 18.2 | Type of Corrosion (Ext SCC/ CUI-SCC) | 
EC driver (climate) M/T/D/S | M | Adjusted Susceptibility | See logic below | Very High | From Insp Confidence table
Coating age (COATAGE) | (Present Year-RPY) | Severity (base on adjusted Susceptibility) | Table 17.3 | High | From Insp Confidence table
Coat Adjustment | See logic below | Line ex Age (LEAGE) | If LIY is not null then Present year-LIY else Present Year-YIS | Med | From Insp Confidence table
Repainted Year (RPY) | Pipe reports | External Process | from Corrosion Study table (default “atmos”) | Low | From Insp Confidence table
Effective External Age | LEAGE-COatAdjust | Damage Factor | POF EC table | Found | From Insp Confidence table
Piping complexity (A/AA/BA) default A | User can change | POF | POF EC table | Last Insp Year (LIY) | From Insp Confidence table (Year of last Insp with VH/H
Insulation Condition default A | Pipe reps (Default Average)/ AA/A/BA |  |  |  | 
External Chloride SCC/CU-SCC
Coating Adjustment
If LEAGE>= COATAGE and CQ=L then 0
else if LEAGE>= COATAGE and CQ=M then min of( 5 or COATAGE)
else if LEAGE>= COATAGE and CQ=H then min of( 15 or COATAGE)
else if LEAGE< COATAGE and CQ=L then 0
else if LEAGE< COATAGE and CQ=M then (min of( 5 or COATAGE)-min of(5, (coatage-LEAGE)
else if LEAGE< COATAGE and CQ=H then (min of(1 5 or COATAGE)-min of(15, (coatage-LEAGE))
If “external process” = “Atmos” and “material code” does not starts with “CS” or “LAS” and “Insulated”=“N” then “Type Of Corrosion” = “External SCC”
If “external process” = “Atmos” and “material code” does not starts with “CS” or “LAS” and “Insulated”=“Y” then “Type Of Corrosion” = “External CU-SCC”
Adjusted Susceptibility
If Found >0 then Adjusted Suceptability= HIGH
elseIf Type of corrosion=Ext SCC then Adjusted Suscep=Susceptability
Else if Type of corrosion=CUI SCC and Piping Compexity and/or Insulation condition = BA then Adjusted Suscep=Susceptability+higher
Else if Type of corrosion=CUI SCC and Piping Compexity and/or Insulation condition = AA then Adjusted Suscep=Susceptability-Lower

## Slide 5
DM Code | Initial Sucep (corrosion Study) | Severity Score (From Corro Study) | Adjusted Susepta | Severity Index | Found | VH | H | M | L | Last Insp Year VH | Reduction Factor | Effective Age | Damage Factor | POF | DM name
 |  |  | See below logic | See below logic |  |  |  |  |  |  |  |  |  |  | 
SCC Damage Mechanism
Adjusted Suceptability
If Found >0 then Adjusted Suceptability= HIGH
Severity Index calculation
If Adjusted Susceptibility = HIGH then Severity Index = 1*Severity Score
Elseif Adjusted Susceptibility = Medium then Severity Index = 0.1*Severity Score
Elseif Adjusted Susceptibility = LOW then Severity Index = 0.01*Severity Score
Elseif Adjusted Susceptibility = NONE then Severity Index = 0*Severity Score
Inserted from corrosion study table based on cluster number

## Slide 6
DM Code | POF (User Assigned in corr study or can add here) | Adjusted POF | Criticality Rank Auto based on POF&COF. (H/MH/M/L) | Criticality Factor (H=1, MH=2, M=3, L=4) (CF) | Found | Last Insp Confidence | Confidence Factor (VH=4, H=3, M=2, L=1) (ICF) | Next Insp Reduction factor NIRF= (CF*ICF) | Max Inspection Interval (Management table) (MI) | Next Rec Inspection frequency NIF =(MI/NIR) years | Last Insp Year (LIY) | Next Insp Year (NIY)= NIF+LIY | DM name
BH | 4 | See below logic | L | 4 | 0 | VH | 4 | 16 | 16 | 1 |  |  | Baffle Hammering
 |  |  | H | 1 |  |  | 4 | 4 | 16 | 4 |  |  | 
Non Trendable Damage Mechanism
Adjusted POF
If Found >0 then Adjusted POF= 1
Else Adjusted POF= POF
HTHA (auto calculation)
If the operating temp is > as per Nelson curve table based on material code then insert a row as HTHA DM
Find the nelson curve temp based on hydrogen partial pressure and material.
Based on the difference between the operating temp and nelson temp Intial POF is selected as per table

## Slide 7
DM Code | POF (Auto calculated) | Adjusted POF | Criticality Rank Auto based on POF&COF. (H/MH/M/L) | Criticality Factor (H=1, MH=2, M=3, L=4) (CF) | Found | Last Insp Confidence | Confidence Factor (VH=4, H=3, M=2, L=1) (ICF) | Next Insp Reduction factor NIRF= (CF*ICF) | Max Inspection Interval (Management table) (MI) | Next Rec Inspection frequency NIF =(MI/NIR) years | Last Insp Year (LIY) or YIS | Next Insp Year (NIY)= NIF+LIY | DM name
Creep |  |  |  |  |  |  |  |  |  |  |  |  | 
Trendable Damage Mechanism
Creep
If the operating temp is > as per table based on material code then insert a row as CREEP DM
Then calculate the stress and accordingly pick the POF as per attached excel sheet (create a form)
Adjusted POF
If Found >0 then Adjusted POF= 1
Else Adjusted POF= POF

## Slide 8
Applicable Fluid as per Table 4.1 |  | Fluid |  | Mass of Inventory Fluid Minv |  | Length of Component, l mm | 
Normal Boiling Point 0C (from table) |  | Operating Temperature Ts K |  | Detection System Rating (Default C) |  | Mass of Fluid in component Mcomp (L*D*Density) | 
Molecular Weight |  | Operating Pressure Ps KPa |  | Fluid Phase at released condition |  | Inner diameter of Component, d mm (OD-2*Thk) | 
Fluid Phase stored |  | Component Type |  | Isolation system rating (default C) |  | Toxic Reference fluid | 
 |  |  |  |  |  | Toxic Fluid % | 
COF Flammable |  | COF Toxic |  | COF Non Flam/Toxic |  | Production Loss | 
COF tab
Production Loss > 10 days A
Production Loss 6-10 days B
Production Loss 1-5 day C
Partial Production Loss D
No Production Loss E

## Slide 9
User
User
User
User
User
User
Inspection Program